شركة مصفاة حمص Homs Refinery Company الموضوع : توريد صودا كاوية صلبة subject : delivery caustic soda ( solid ) مديرية :الطاقة by: Directorate of energy

| 1- الكمية :412 طن 2-المواصفات الفنية : - النقاوة ( التركيز ) : 98 % كحد أدنى - الشكل الفيزيائي : صودا صلبة بأنواعها (صب أو قشور ) 3- التراكيز القصوى للشوائب محسوبة على أساس 100% ماءات الصوديوم : - الكربونات : 10000 جزء في المليون كحد أقصى على شكل Na2CO3 - الكبريتات : 1500 جزء في المليون كحد أقصى على شكل Na2SO4 - الكلوريدات : 3000 جزء في المليون كحد أقصى على شكل NaCl - الحديد : 60 جزء في المليون كحد أقصى - المواد غير الذوابة في الماء :500 جزء في المليون كحد أقصى - السيلكا : 100 جزء في المليون كحد أقصى على شكل SiO2 4- التغليف : في حال الصلبة : صب يجب أن تكون المادة معبأة ضمن براميل حديدية جديدة محكمة الإغلاق وملائمة للتخزين . وزن البرميل 200 – 400 كغ . ب – في حال الصلبة قشور يجب أن تكون معبأة في أكياس من مادة البولي ايتلين وأن يكون الوزن من (25-50 ) كغ للكيس الواحد موضوعة على طبليات خشبية مغلفة بطبقة من البلاستيك وان تكون الاكياس مناسبة للتداول و التخزين 5- التوريد : يجب أن يتم التوريد على دفعة واحدة 6- يتم استلام المادة الموردة بعد تحليلها في مخابر مصفاة حمص للتأكد من مطابقتها لدفتر الشروط الفنية المطلوبة . 7- العرض الفني يجب أن يتضمن النشرات الفنية الخاصة بالمادة مع بيان بلد المنشأ واسم الصانع الأصلي للمادة. انتهى | 1 - Quantity : 412 Tons 2 – Specifications: - Purity : 98% min - Physical form : soda (solid or flakes) 3 – Max . Limits of impurities based on 100% NaOH : -Carbonate : 10000 ppm as Na2CO3 Max - Sulphate : 1500 ppm as Na2SO4 Max - Chloride : 3000 ppm as NaCl Max - Iron : 60 ppm Max - Insoluble matters in water : 500 ppm Max - Silica : 100 ppm as SiO2 Max 4 – Packing a- In case of soda: solid New steel drums , tightly closed , suitable for storage , Each one contains 200 – 400 kg b- In case of soda: flakes It should be packed in bags made of Polyethylene, and the weight of each bag should be (25-50) kg. on wooden pallets covered with plastic layer the bags and pallets should be suitable for handling and storage 5 – Delivery : One shipment 6 – Supplied material will be accepted after testing in Homs Refinery Lab to assure its conformity to required specification . 7 – The technical offer shall be contained the technical specification of the offered material , the original manufacture s name , country. End |
| --- | --- |

م0 طارق الابراهيم                                                            م . حسان عبدان                                  ك . علي العكاري

Tel:+963 31 470101(1-2-3)/516401 Fax:+963 31 516410/516411

Email:homs-refine@mail.sy P.O. Box:352/355 Homs-Syria