| دفتر الشروط الفنية لتوريد مجموعة وسائط لوحدة إنتاج النتروجين 1200ب 1 – وصف عام : * تشكل وحدة PSA الوحدة الأساسية في وحدة النتروجين /1200ب / تتألف من مجموعتي أبراج متماثلتين متناوبتين بالعمل(١ دقيقة + ١ دقيقة ) . كل منهما تتألف من مرحلتين المرحلة الأولى عمود فيه وسيط activated alumina لتجفيف الهواء وازالة الرطوبة حتى 5 ppm والمرحلة الثانية عمودين فيهما الوسيط الأساسي (carbon molecular sieve ) مهمته امتزاز جزيئات الأوكسجين من الهواء المجفف الداخل عن طريق مسام قطرها يتوافق مع قطر جزيئات الأوكسجين لنحصل على النتروجين النقي 99.99 % . *وحدة NDU هي وحدة تجفيف منتج النتروجين النهائي تتألف من عمودين دورة العمل لهما ( 5دقائق( وفيهما وسيط التجفيف Molecular sieve type 13X 2 – الهدف : توريد الوسائط المذكورة واصلة أرض الشركة العامة لمصفاة حمص بغية استمرار عمل الوحدة. 3– الكميات المطلوبة : 3-1- Activated alumina : كغ6000 3-2- Carbon molecular sieve : 9000 كغ 3-3- Molecular sieve type 13X 550 كغ ٤ - المواصفات الفنية : 4-1-activated alumina 4-1-1- شكل الحبيبات : كروي . 4-1-2- النوع :1S -1 SIALCA 4-1-3- الحجم : ٣ - ٥ مم 4-1-4- الكثافة الحجمية : gms/L 810±15 4-1-5- الضياع بالاحتكاك : 0.18 % 4-1-6- حجم المسام (cc/gms) : 0.4 4-1-7- قدرة امتصاص الرطوبة عند درجة حرارة 30 c° و رطوبة نسبية 60% : 19.8 % ( الأفضلية للقيمة الأعلى ) 4-1-8- الممانعة لقوة التحطم : 95.2 % 4-1-9- السطح النوعي (m2/gm): 280 4-1-10- الرطوبة الحرة % : 1.08 4-1- 11- التركيب : : AL2O3 94.1 % N2O2 : 0.06 % Fe2O : 0.05 % SiO2 : 0.04 % 4-2- carbon molecular sieve (MSC 3KT_172) : 4-2-1- شكل الحبيبات : اسطواني 4-2-2- اللون : أسود 4-2-3- حجم الحبيبات الوسطي(1.18 - 2.8 مم ) % : 99.9 4-2-4- الفاقد بالتجفيف % : 0.1 4-2-5- الكثافة الحجمية(g/ml ) : 0.694± 0.05 4-2-6- القساوة % : 99 4-2-7- فعالية ال PSA بشروط عمل( N2 99 % ،ودرجة حرارة 30 مْ وضغط 6.9 بار ودورة العمل 60 ثانية ) كما يلي : نسبة فصل النتروجين من الهواء 40.3% وزنا إنتاجية النتروجين 205.4 Nm3/hr.ton (الأفضلية للقيمة الأعلى). Molecular sieve type 13X 4-3- 4-3-1 - شكل الحبيبات : كروي 4-3-2 - حجم الحبيبات : 3-5 مم 4-3-3 - الممانعة للتحطم : 90.4 % 4-3-4- الكثافة الحجمية (gm/l) : 630 ± 15 4-3-5- الفاقد بالاحتكاك % : 0.1 4-3-6- قدرة امتصاص الرطوبة عند درجة حرارة 30 C° : عند رطوبة نسبية 75% 26.5% عند رطوبة نسبية 15% 22.6% ( الأفضلية للقيمة الأعلى ) 5- الوثائق المطلوبة : 5-1 - على المتعهد أن يقدم شهادة اختبار معتمدة من الشركة المصنعة مذكور فيها كمية الشحنة الموردة وكمية العينة المختبرة ونتائج الاختبار بما فيها المواصفات الفنية لكل وسيط . 5-2- على المتعهد أن يقدم وثيقة تضمن العمر التشغيلي لكل وسيط كما يلي : Activated alumina ٥سنوات CMS ٩ سنوات Molecular sieve 13X٥سنوت 5-3 - على العارض الالتزام بتقديم الوثائق المطلوبة كشرط أساسي لاستلام المواد مع ذكر بلد المنشأ . ٦ - متطلبات عامة : 6-1- على العارض توريد الوسيط في أوعية محكمة الإغلاق (براميل بلاستيكية أو معدنية) وعلى كل برميل لصاقة مكتوب عليها نوع الوسيط و كمية الوسيط فيه . 6-2- الشحنة الموردة غير قابلة للتجزئة . 6-3 - مدة التوريد 120يوم . 6-4- مدة الضمان سنة تشغيلية كاملة . 6-5- إذا فشل الوسيط بأدائه خلال سنة الضمان فيجب على العارض استبدال هذا الوسيط بشحنة وسيط كاملة مجانية . 6-6- إذا فشل الوسيط بأدائه بعد انقضاء سنة الضمان فيجب على العارض أن يقدم مبلغا ماليا يقدر كما يلي: عدد السنوات المتبقية من العمر التشغيلي الذي ضمنه العارض منسوبا إلى العمر التشغيلي الذي ضمنه العارض ومضروبا بسعر الوسيط . | Book of Technical conditions To supply Set of catalysts For Nitrogen generation Unit 1200B 1- General demonstration : * PSA is the critical unit of nitrogen unit /1200B /and consists of twin tower system in swing operation (1min+1min) . The one tower system consists of two portions lower portion is a tower contain activated alumina for drying air and eliminate moisture up to 5ppm and upper portion is two towers contain the main catalyst (carbon molecular sieve) It adsorbs oxygen molecules from the dried air by pores have diameter is in the same range as those of oxygen molecules to get pure nitrogen 99.99% . * NDU unit is the drying unit of nitrogen product , consists of two towers of cycle time (5 min) and contain drying catalyst Molecular sieve type 13X 2 - Target : To supply and delivery of these catalysts to the land of the general company of Homs refinery , to achieve continuance of unit operation . 3- Required quantities : 3-1- Activated alumina : 6000kg 3-2- Carbon molecular sieve : 9000 kg 3-3- Molecular sieve type 13X : 550 kg 4- Technical specifications : 4-1- Activated alumina : 4-1-1- particle shape: spherical beads . 4-1-2- grade : SIALCA 1S-1 4-1-3- Size : 3-5 mm 4-1-4- bulk density gms/L: 810 ± 15 . 4-1-5- Attrition loss : 0.18% 4-1-6- pore volume (cc/gms): 0.4 4-1-7- Water adsorption capacity at 30 c° , at 60% RH : 19.8 % ( the preference is the greater amount ) . 4-1-8- Bed crushing strength : 95.2% 4-1-9- Surface aria (m2/gm): 280 4-1-10- Free moisture %: 1.08 4-1-11- composition : AL2O3 : 94.1% N2O2 : 0.06% Fe2O: 0.05% SiO3%: 0.04% 4-2- Carbon molecular sieve (MSC 3KT-172): 4-2-1- particle shape : cylindrical 4-2-2- Color : black 4-2-3- particle size (1.18- 2.8 mm) %: 99.9 4-2-4- Attrition Loss %: 0.1 4-2-5- Bulk density(g/ml): 0.694 ± 0.05 4-2-6- Hardness % : 99 4-2-7- PSA performance at (99% N2 and temperature 30Cͦ , pressure 6.9 bar ,cycle time 60sec) as follow : Recovery nitrogen / air 40.3 % wt Productivity N2 205.4 Nm3/hr.ton (the preference is the greater amount) . 4 -3-Molecular sieve type 13X: 4-3-1- Particle shape: spherical Beads. 4-3-2- particle size :3-5mm 4-3-3- Crushing bed strength : 90.4 % 4-3-4- Bulk density (gm/l): 630± 15 4-3-5 - Attrition loss%: 0.1 4-3-6 - Adsorption capacity at 30 C° : At relative humidity 75% 26.5% At relative humidity 15% 22.6% ( the preference is the greater Amount ) . 5- Required certificates : 5-1 - Contractor must provide legalized test certificate from manufacturer company specified in it quantities of supply shipment and tested sample and test results including technical specifications of each catalyst . 5-2- Contractor must provide indent insures the operating life of each catalyst as follows: Activated alumina : 5 years CMS :9 years Molecular sieve 13X : 5 years 5-3- Bidder must abide by providing all certificates as prerequisite for receipt procedures of these catalysts in addition that the country of origin must be specified . 6- General requirements : 6-1- Bidder must supply catalysts packed in air tight containers ( plastic or mineral barrels ) and each barrel hanging on it a sticker specified in it type and weight of catalyst . 6-2- The supplied shipment is indivisible . 6-3- Supplying duration is 120 days. 6-4- period warranty is one working year . 6-5- Bidder must replace the whole shipment of any catalyst by a new catalyst shipment if the performance of catalyst has a problem during the warranty period . 6-6- If the performance of the catalyst has a problem after ending of the warranty period, the bidder must repay as follow : the rate of remaining years number of the operating life that is insured by the bidder to the operating life number insured by the bidder multiplied by the catalyst price . |
| --- | --- |

أعضاء اللجنة الفنية

عضوا                                 عضوا                              رئيس اللجنة

م. فراس عباس                        م. لبنى ونوس                          م. مهند صارم